## Slide 1: STM Study of Mott Gap in TaS2
Xin-Yang Zhu, Shao-Chun Li
March 2nd, 2018

## Slide 2
LHB
Three-band model v.s. one-band model?
Single-particle DOS in a Fermi liquid
as a function of the electron filling n
Three-band model

## Slide 3: Research Background
Mottness Collapse in 1T-TaS2-xSex Transition-Metal Dichalcogenide: An Interplay between Localized and Itinerant Orbitals
Shuang Qiao, …, Jian Wu, Yayu Wang, Zheng Liu, Phys Rev X 7, 041054 (2017)

## Slide 4: Research Background
Mottness Collapse in 1T-TaS2-xSex Transition-Metal Dichalcogenide: An Interplay between Localized and Itinerant Orbitals
Shuang Qiao, …, Jian Wu, Yayu Wang, Zheng Liu, Phys Rev X 7, 041054 (2017)

## Slide 5: Research Background
Mottness Collapse in 1T-TaS2-xSex Transition-Metal Dichalcogenide: An Interplay between Localized and Itinerant Orbitals
Shuang Qiao, …, Jian Wu, Yayu Wang, Zheng Liu, Phys Rev X 7, 041054 (2017)

## Slide 6: Clean Surface and STS
200mV 100pA 50X50nm
500mV 200pA

## Slide 7: STS Line Map Taken at the Clean Surface
STS line map
1V, 200pA, modulation: 15mV

## Slide 8: STS Taken at Surface Defects

## Slide 9: TaS2 Surface with K Doping
0 ML
0.016 ML
0.02 ML
0.044 ML
0.053 ML
0.065 ML
0.07 ML
0.12 ML
0.18 ML
0.24 ML
0.32 ML
0.047 ML

## Slide 10: STS Spectra with K Doping

## Slide 11: Spectral Feature Evolution upon K Doping
?
?

## Slide 12: Long-range Coherence of CDW
CDW
FFT
Filtered
IFFT

## Slide 13: Long-range Coherence of CDW

## Slide 14: Summary
随着电子的掺杂，费米能级开始向UHB移动，同时两个Hubbard带并没有明显的变化
当Fermi能级移动到上hubbard处时，能带突然发生变化，Mott gap消失，成为金属态
金属态依然具有长程的电荷密度波序
问题：

## Slide 15
K: 1s
K: 17s
K: 17s
+ Pulse

## Slide 16
1V 100pA
100 X 100nm